Comparison between NiMH, Lead Acid and Li-Ion Battery at Similar Energy Level (360 Wh)

| Battery type | Weight | Volume | Energy Density by weight / size | Cost ($/wh) |
| --- | --- | --- | --- | --- |
| SLA (3x12V 10Ah) | 10 kg | 3270 cm3 | 36 wh/kg | 0.11 wh/cm3 | $0.20 /wh |
| NiMH (36V10Ah) | 5.5 kg | 2430 cm3 | 65 wh/kg | 0.15 wh/cm3 | $1.00 / wh |
| Poly Li-Ion (8Ah) | 1.75 kg | 1340 cm3 | 170 wh/kg | 0.23 wh/cm3 | $1.25/wh |
| Poly Li-Ion (10Ah) | 2.15 kg | 1613 cm3 | 170 wh/kg | 0.23 wh/cm3 | $1.20/wh |

Cost is estimated based on retail price published from www.batteryspace.com, in April 2007,  which may change without notice