| Polymer Lithium-ion battery Product Specification | Doc. No. |  |  |
| --- | --- | --- | --- |
|  | Edition No. |  | 2.0 |
|  | # Sheet |  | 1 |
| - Scope This product specification describes 063465 polymer lithium-ion battery. Please use the test methods that recommend in this specification. If you have any opinions or advices about the test items and methods, please contact us. - Product Type, Model and Dimension 2.1 Type：Polymer lithium-ion battery 2.2 Model： 063465 2.3 Dimension(Thickness×Width×Length，mm3)： 6.0×34.0×65.5 - Specification Item; Specifications; Remark. Nominal Capacity; 1400 mAh; 0.2C5A discharge. Nominal Voltage; 3.7V; Average Voltage at 0.2C5A discharge. Charge Current; Standard：0.2 C5A；Max：1C5A; Working temperature：0～40℃. Charge cut-off Voltage; 4.20±0.03V. Discharge Current; Max：2C5A; Working temperature：-20～60℃. Discharge cut-off Voltage; 2.75V. Impedance; ≤ 40 mΩ; AC 1KHz after 50% charge. Weight; Approx: 28 g. Storage temperature; <1个月; -20～60℃; Best 20±5℃ for long-time storage. <3个月; -20～45℃. <12个月; -20～20℃. Storage humidity; 65±20% RH. - General Performance Definition of Standard charging method：At 20±5℃，charging the cell initially with constant current 0.2C5A till voltage 4.2V, then with constant voltage 4.2V till current declines to 0.05C5A. Item; Test Methods; Performance. 4.1 0.2C Capacity; After standard charging, laying the battery 1h, then discharging at 0.2C5A to voltage 2.75V, recording the discharging time.; ≥300min. 4.2 1C Capacity; After standard charging, laying the battery 1h, then discharging at 1C5A to voltage 2.75V, recording the discharging time.; ≥51min. 4.3 Cycle Life; Constant current 1C5A charge to 4.2V, then constant voltage charge to current declines to 0.05C5A, stay 5min，constant current 1C5A discharge to 2.75V，stay 5min. Repeat above steps till continuously discharging time less than 36min.; ≥300 times. 4.4 Storage; 20±5℃, After standard charging, laying the battery 28days, discharging at 0.2C5A to voltage 2.75V, recording the discharging time.; ≥240min. |
| Polymer Lithium-ion battery Product Specification | Doc. No. |  |  |
|  | Edition No. | 2.0 |  |
|  | Sheet | 2 |  |
| - Environment Performance Item; Test Methods; Performance. 5.1High temperature; After standard charging, laying the battery 4h at 60℃, then discharging at 0.2C5A to voltage 2.75V, recording the discharging time.; ≥270min. 5.2 Low temperature; After standard charging, laying the battery 4h at 0.2C5A, then discharging at 0.2C5A to voltage 2.75V, recording the discharging time.; ≥210min. 5.3 Constant humidity and temperature; After standard charging, laying the battery 48h at 40±2℃, RH 93±2%.; No influence to batteries' appearance. 0.2C5A discharging time ≥270 min. 5.4 Temperature shock; After standard charging, battery stored at -20℃ for 2 hours, then stored at 50℃ for 2 hours. Repeat 10 times.; No electrolytes leakage. 5.5 Vibration; After standard charging, put battery on the vibration table. 30 min experiment from X,Y,Z axis. Scan rate: 1 oct/min; Frequency 10-30Hz, Swing 0.38mm; Frequency 30-55Hz, Swing 0.19mm.; No influence to batteries' eletrochemical character and appearance.. 5.6 Collision; After vibration test, batteries were laying on the vibration table about X, Y, Z axis. Max frequency acceleration: 100m/s2; collision times per minutes: 40~80; frequency keeping time 16ms; all collision times 1000±10.; No influence to batteries' eletrochemical character and appearance.. - Safety Test Test conditions：The following tests must be measured at flowing air and safety protection conditions. All batteries must standard charge and lay 24h. Item; Test Methods; Performance. 6.1 Over charging; At 20±5℃, charging batteries with constant current 3C5A to voltage 5V, then with constant voltage 5V till current decline to 0. Stop test till batteries’ temperature 10℃ lower than max temperature.; No explosion or fire. 6.2Over discharging; At 20±5℃, discharge battery with 0.2C5A continuously 12.5h.; No explosion or fire. 6.3 short-circuit; At 20±5℃, connect batteries’ anode and cathode by wire which impedance less than 50mΩ, keep 6h.; No explosion or fire. 6.4 Nail pierce; At 20±5℃, φ3mm nail pierce the battery, keep 6h.; No explosion or fire. 6.5 Drop; Random drop the battery from 10m height onto concrete one times.; No explosion or fire. 6.6 Extrusion; At 20±5℃, put the battery in two parallel steal broad, add pressure 13kN.; No explosion or fire. 6.7 Thermal shock; Put the battery in the oven. The temperature of the oven is to be raised at 5±1℃ per minute to a temperature of 130±2℃ and remains 60 minutes.; No explosion or fire. |

| Polymer Lithium-ion battery Product Specification | Doc. No. |  |
| --- | --- | --- |
|  | Edition No. | 2.0 |
|  | Sheet | 3 |
| - Cautions - Cautions of batteries’ operation The batteries must be careful of proceed the operation for it’s soft package. ⒈ Aluminum packing materials The aluminum packing material was easily damaged by the sharp edge part, such as nickel-tabs. ⑴ forbid to use the sharp part touching the battery; ⑵ should cleaning working condition, avoiding the sharp edge part existence; ⑶ forbid to pierce the battery with nail and other sharp items; ⑷ the battery was forbidden with metal, such as necklace, hairpin etc in transportation and storage. ⒉ Sealed edge Sealing edge is very easily damaged and don’t bend it. ⒊ Folding edge The folding edge is formed in batteries’ processes and passed all hermetic tests, don’t open or deform it. ⒋Tabs The batteries’ tabs are not so stubborn especially for aluminum tabs. Don’t bend tabs. ⒌Mechanical shock Don’t fall, hit, bent the batteries’ body. ⒍Short-circuit Short-circuit is strictly prohibited. It should damage batteries badly. - Standard Test Environment for polymer lithium-ion batteries Environment temperature: 20±5℃ Humidity: 45-85% - Cautions of charge & discharge ⒈ charge Charging current should be less than values that recommend below. Higher current and voltage charging may cause damage to cell electrical, mechanical, safety performance and could lead heat generation or leakage. ⑴ Batteries charger should charging with constant current and constant voltage mode; ⑵ Charging current should be less than 1C5A; ⑶ Temperature 0～45℃ is preferred when charging; ⑷ Charging voltage must be less than 4.23V. ⒉ discharge ⑴ Discharging current must be less than 2C5A; ⑵ Temperature 20～60℃ is preferred when discharging; ⑶ Discharging voltage must not be less2.75V. ⒊ over-discharge It should be noted that the cell would be at an over-discharge state by its self-discharge. In order to prevent over-discharge, the cell shall be charged periodically to keeping voltage above 3.0V. Over-discharge may cause loss of cell performance. It should be noted that the cell would not discharge till voltage less than 2.5V. - Storage of polymer lithium-ion batteries The environment of long-time storage: Temperature: -20～35℃; Humidity: 45-75%; Batteries were 40～60% charged. - Transportation of polymer lithium-ion batteries The batteries should transportation with 10～50% charged state. |  |  |
| Polymer Lithium-ion battery Product Specification | Doc. No. |  |
|  | Edition No. | 2.0 |
|  | Sheet | 4 |
| - Others Please note cautions below to prevent cells’ leakage, heat generation and explosion. Prohibition of disassembly cells; Prohibition of cells immersion into liquid such as water or seawater; Prohibition of dumping cells into fire; Prohibition of using damaged cells. The cells with a smell of electrolyte or leakage must be placed away from fire to avoid firing. In case of electrolyte leakage contact with skin, eye, physicians shall flush the electrolyte immediately with fresh water and medical advice is to be sought. |  |  |